**DESCRIPTION**

MT-A7772 is a high strength aluminum foil tape coated with a superior performance flame retardant solvent acrylic adhesive. The foil material allows maximum conformability in vapor sealing fiberglass duct boards and FSK systems. A low moisture vapor transmission rate offers outstanding sealing and patching performance, providing an excellent vapor seal. This tape features good aging resistance both indoors and outdoors. A superior quick stick at normal operating temperatures and great performance at low temperatures.

**APPLICATIONS**

* HVAC industry for sealing joints and seams of foil-faced insulation materials
* Joining and sealing flexible air duct seams and connections
* Seaming foil and FSK insulations

**FEATURES & BENEFITS**

* UL723

CAN/ULC-S102

SIZES

* 48, 72 mm x 150 ft.
* 48, 72 mm x 300 ft.

COLORS

* Silver

PRODUCT CONSTRUCTION

|  |  |
| --- | --- |
| Backing | 1.6 mils Aluminum foil |
| Adhesive | Flame retardant solvent acrylic |

TECHNICAL DATA

|  |  |
| --- | --- |
| Total Thickness | 3.35 mils |
| Tensile | 10.2 lbs./in. |
| Adhesion | ≥50 oz./in. |
| Application temperature | -4°F to 104°F (-20°C to 48°C) |
| Service temperature | -37°F to 248°F (-35°C to 120°C) |